## Slide 1: DW field-switching micromag and fitting results
updated 25/11/21

## Slide 2: BLS notes: fitting eqn
Appl. Phys. Lett. 120, 112405 (2022); doi: 10.1063/5.0083583
DE  1
BV  0
Fitting parameters
Determined through FMR
Less valid for thicker films

## Slide 3: Non-device ways to measure Aex
Neutron scattering  gold standard
Temperature dependent magnetometry
Perpendicular standing spin waves (PSSWs)
  Brillouin light scattering (BLS)
  Ferromagnetic resonance (FMR)
Damon-Eschbach and backscattering mode dispersion
  BLS
  FMR in devices
Problem: Cannot measure in films less than 10 nm

## Slide 4: Output and fitting using equation (2 kHz sampling)
Fitted:
Aex = 1.739e-06 erg/cm
w_dw = 13.808 nm
Delta = 144.449
Generated:
Aex = 1.776e-06 erg/cm
w_dw = 12.7 nm
Delta = 145.95
Fitted:
Aex = 1.929e-06 erg/cm
w_dw = 13.482 nm
Delta = 152.126
Generated:
Aex = 2.012e-06 erg/cm
w_dw = 12.7 nm
Delta = 155.362
P(H)
H (Oe)
P(H)
H (Oe)

## Slide 5: Output and fitting using equation (1 GHz sampling)
Fitted:
Aex = 1.711e-06 erg/cm
w_dw = 12.423 nm
Delta = 143.253
Generated:
Aex = 1.776e-06 erg/cm
w_dw = 12.7 nm
Delta = 145.95
P(H)
H (Oe)

## Slide 6: Mumax output
P(H)
H (Oe)
Aex=1.6E-6
Aex=1.9E-6
Aex=1.77E-6
Mumax:
Aex = 1.776e-06 erg/cm
sampling rate = 1 GHz
Ki = 2.48 erg/cm2
Ku1 = Ki/t_fl (seems to be too large)

## Slide 7: Mumax best fitting attempt (scipy)
Fitted:
Aex = 1.604e-06 erg/cm
w_dw = 11.340 nm
Delta = 173.071
f_att = 5.079 GHz
Hk = 2817.147 Oe
Mumax:
Aex = 1.776e-06 erg/cm
f_att = 5.079 GHz
sampling rate = 1 GHz
Ki = 2.48 erg/cm2
Ku1 = Ki/t_fl (seems to be too large)
P(H)
H (Oe)
Fitting variables:
Aex
delta (w_dw = |diameter*delta|)
f_att
Hk

## Slide 8: Next (10/18/2025)
Error propagation for fitting
  Look into more advanced fitting packages (lmfit)
Domain wall length calculation
Physical measurements

## Slide 9: Mumax fitting attempt (lmfit)
Mumax:
Aex = 1.776e-06 erg/cm
f_att = 5.079 GHz
sampling rate = 1 GHz
Ki = 2.48 erg/cm2
Ku1 = Ki/t_fl (seems to be too large)
Fitted:
Aex = 1.604e-06 erg/cm
w_dw = 11.340 nm
Delta = 173.071
f_att = 5.079 GHz
Hk = 2817.147 Oe
P(H)
H (Oe)
Fitting variables:
Aex
delta (w_dw = |diameter*delta|)
f_att
Hk

## Slide 10: DW length results